## Slide 1
FBI·G4
FBI·G3
FBI·G2
FBI·G1
Compound | lema (nm) |  | Dl (nm) |  |  |  | (M-1 cm-1) |  | (M-1·cm-1) |  | (Å2) |  | Kad (M-1)
 | Gn | Gn·Ba2+ |  |  | Gn | Gn·Ba2+ | Gn | Gn·Ba2+ | Gn | Gn·Ba2+ | Gn | Gn·Ba2+ | 
G2 | 622 | 552 | 70 | 210.6 | 0.23 | 0.55 | 5,990 | 16,564 | 26,044 | 30,117 | 1.00 | 1.15 | 1.3·106
AAN155 | 502 | 618 | 116 |  | 0.02 | 0.08 | 254 | 1000 | 12,705 | 12,750 | 0.49 | 0.49 | 4.3·105
AAN160 | 500 | 590 | 90 |  |  |  |  |  | 10,301 | 10,822 |  |  | 4.7·106
Compound | lema (nm) |  | Dl (nm) |  |  |  |  |  |  |  |  |  | Kad (M-1)
 | Gn | Gn·Ba2+ |  |  | Gn | Gn·Ba2+ | Gn | Gn·Ba2+ | Gn | Gn·Ba2+ | Gn | Gn·Ba2+ | 
G2 | 622 | 552 | 70 | 210.6 | 0.23 | 0.55 | 5,990 | 16,564 | 26,044 | 30,117 | 1.00 | 1.15 | 1.3·106
AAN155 | 502 | 618 | 116 |  | 0.02 | 0.08 | 254 | 1000 | 12,705 | 12,750 | 0.49 | 0.49 | 4.3·105
AAN160 | 500 | 590 | 90 |  |  |  |  |  | 10,301 | 10,822 |  |  | 4.7·106
a Emission wavelengths λem at a lexc_max .b Peak discrimination factors (fλ) with respect to unbound fluorophores Gn at λem. c All values for Quantum yields фλ , molecular brightness of the fluorescent emissions (Bλ), molar extinction coefficient at l(G2) =325 nm; AAN155 and AAN160 at their isosbestic point l(AAN155)= 365 nm; l(AAN160)= 370 nm. d Ka with barium perchlorate in acetonitrile at 298 K using Nelder-Nelder mead fitting on the 300-500 nm spectral region.
AAN160
AAN-155
FBI-G2

## Slide 2
AAN155 absorption (1E-5M)
AAN155 emission (1E-5M)
Excitation at 365 nm