## Slide 1
Coverage (mol/cm2) = A/(e*1000)
Materna, K. L.; Jiang, J.; Crabtree, R. H.; Brudvig, G. W., Silatrane Anchors for Metal Oxide Surfaces: Optimization for Potential Photocatalytic and Electrocatalytic Applications. ACS Applied Materials & Interfaces 2019, 11 (6), 5602-5609.
1 nmol/cm2 = 6.023E14 molecules/cm2

## Slide 2
e (469 nm)=8801.47 M-1cm-1
A (469 nm)=0.00291299
Coverage = A/(e*1000) = 3.31E-10 mol/cm2 = 1.99E14 molecules/cm2
Ru-silatrane on quartz

## Slide 3
e (469 nm)=8801.47 M-1cm-1
A (469 nm)=0.00247252
Coverage = A/(e*1000) = 2.81E-10 mol/cm2 = 1.69E14 molecules/cm2
Ru-silatrane on ITO

## Slide 4
e (469 nm)=8801.47 M-1cm-1
Ru-silatrane/APTES-silatrane (1/1) on ITO

## Slide 5
e (469 nm)=8801.47 M-1cm-1
Ru-silatrane/APTES-silatrane (1/1) on ITO

## Slide 6
Ru-silatrane on quartz
Ru-silatrane on quartz
Ru-silatrane/PTES silatrane 1/10 on ITO
Ru-silatrane PTESsilatrane 1/1 on ITO
Ru-silatrane on ITO